## Slide 1
Phase Diagrams
Dr. J. Venkatramani
219-B
venkatramani@iiitdm.ac.in

## Slide 2
Terminology
Solute
Solvent
Component
System

## Slide 3
Solubility Limit
Water continues to dissolve sugar till a certain limit called solubility limit.
Beyond this limit, sugar does not dissolve and thus, remain as a separate substance within the sugar–water solution.
Solubility is temperature dependent.
The solubility of sugar (C12H22O11) in a sugar–water syrup.

## Slide 4
Definition of a phase
Homogeneous portion of a system that has uniform physical and chemical characteristics.
Every pure material is considered to be a single phase system.
When two phases exist in a system, they can differ in either physical properties or in chemical properties or in both.
Examples: Sugar–Water solution + Solid sugar; Ice + Water
Existence of a substance in two or more polymorphic forms, like FCC, BCC is possible. Then, each of these structures within the substance is a phase.
Single phase systems are termed “homogeneous”, while the ones with more than one phase are termed “mixtures” or “heterogeneous”. Alloys, ceramic, polymeric and composites systems are heterogeneous.

## Slide 5
Phase Equilibria
Free Energy: F = E–TS, where, E is the internal energy of the system, T the absolute temperature and S, the entropy.
A system is said to be in equilibrium when its free energy is at a minimum for a given pressure, temperature and composition.
Phase equilibrium refers to the equilibrium of systems with more than one phases. Look at the figure showing sugar–water solution + solid sugar system at different temperatures and compositions.
Phase equilibrium is relevant even in systems having only solid phases.
Non–equilibrium or metastable states exist in solid phase systems.

## Slide 6
One Component Phase Diagrams (Unary Phase Diagrams)
Phase diagram of a pure substance. Only pressure and temperature are the variables.
Triple point.
Is there any other variable that the phase diagram of a pure substance will depend on?

## Slide 7
Binary Phase Diagrams
Temperature and composition are variables. Pressure is held constant (normally at 1 atm).
Cu – Ni System: an isomorphous system (no solubility limit).
Complete solubility below 10800C. They have same crystal structure (FCC), nearly identical atomic radii and electronegativities and similar valences – which are all requirements for substitutional type of defects.
Metallic solid solutions are commonly designated by lowercase Greek letters α, β, γ etc.
The phase boundary separating (α + L) and L is called liquidus. The one separating (α + L) and α is called Solidus.
The intersection points of the these boundaries are the respective melting points.

## Slide 8
Binary Phase Diagrams – Interpretation
A horizontal line in the phase diagram is an isotherm, also called Tie line.
Draw a tie line passing through the point B.
The composition of L phase is given by CL and that of α is given by Cα.
To find phase fractions
Hint: Use the distance from point B to either of the phase boundaries.
Phase fraction of α phase = R/(R+S) and for L phase is S/(R+S).
Equivalently,

## Slide 9
Binary Phase Diagrams – Interpretation
For multi–phase alloys (more than two), volume fractions are preferred.

## Slide 10
Development of Microstructure – Equilibrium Cooling

## Slide 11
Development of Microstructure – Nonequilibrium Cooling

## Slide 12
Mechanical Properties of Isomorphous Alloys

## Slide 13
Binary Eutectic Systems – Cu + Ag
Solubility limit
Solidus
Liquidus
Solvus
Melting temperature
Cooling and heating
Eutectic Reaction
Eutectic Isotherm
Eutectic system

## Slide 14
Binary Eutectic Systems – Pb + Sn
Solubility limit
Solidus
Liquidus
Solvus
Melting temperature
Cooling and heating
Eutectic Reaction
Eutectic Isotherm
Eutectic system

## Slide 15
Lead–free solders – Sn + Bi
Ternary alloys as lead–free solders.
* Stands for eutectic systems.
Various alloy compositions for lead–free solders.

## Slide 16
Microstructure in Eutectic Alloys

## Slide 17
Microstructure in Eutectic Alloys
Dark layers are of α–phase and bright layers are of β–phase.

## Slide 18
Microstructure in Eutectic Alloys

## Slide 19
Microstructure in Eutectic Alloys – Phase Fractions

## Slide 20
Binary Eutectic Systems – Pb + Sn
Compute all the phase fractions for a 40% tin and 60% Pb alloy at a temperature just below 1830 C.

## Slide 21
Equilibrium Diagrams Having Intermediate Phases or Compounds

## Slide 22
Equilibrium Diagrams Having Intermediate Phases or Compounds

## Slide 23
Eutectoid and Peritectic Reactions

## Slide 24
Congruent Phase Transformations
Ni–Ti system

## Slide 25
Gibbs Phase Rule
P + F = C + N
P → Number of phases in the system F → Number of degrees of freedom
C → Number of components N → Number of non–compositional variables

## Slide 26
Failure of Liberty Ships

## Slide 27
Iron – Carbon System
Fe – Fe3C

## Slide 28
Microstructure evolution in Fe – Fe3C systems
Pearlite
The darker layers are of Fe3C and the lighter ones are of α

## Slide 29
Microstructure evolution in Fe – Fe3C systems
Pearlite
The darker layers are of Fe3C and the lighter ones are of α

## Slide 30
Hypoeutectoid alloys
γ → α + γ → α + pearlite
α phase will start forming along γ grain boundaries.
Final structure consists of pro–eutectoid and eutectoid ferrite micro–constituents.

## Slide 31
Hypoeutectoid alloys
Final structure consists of pro–eutectoid and eutectoid ferrite micro–constituents.

## Slide 32
Hypereutectoid alloys
Final structure consists of pro–eutectoid and eutectoid cementite (Fe3C) micro–constituents.

## Slide 33
Finding compositions and phase fractions

## Slide 34
Adding other alloying elements to Fe – C system

## Slide 35
How many kilograms of nickel must be added to 1.75 kg of copper to yield a liquidus temperature of 13000C? How many kilograms of nickel must be added to 5.43 kg of copper to yield a solidus temperature of 12000C?
Concept Check?

## Slide 36
Consider a hypothetical eutectic phase diagram for metals A and B. Assume that: (l) α and β phases exist at the A and B extremes of the phase diagram, respectively; (2) the eutectic composition is 36 wt% A–64 wt% B; and (3) the composition of the α phase at the eutectic temperature is 88 wt% A–12 wt% B and that of β phase is 8 wt% A–92 wt% B. Melting temperatures of A and B are 3270C and 2320C. The eutectic phase transformation occurs at 1830C. Construct the eutectic phase diagram. Determine what composition of the alloy will yield primary β and eutectic β phase fractions of 0.367 and 0.401, respectively.
Concept Check?