## Slide 1
Electrical and Electronic Properties
Dr. J. Venkatramani
219-B
venkatramani@iiitdm.ac.in

## Slide 2
OHM’s Law
V = IR

## Slide 3
Electrical Conductivity
An equivalent statement of Ohm’s law:
,
Where, J is the current density;
E is the electric field intensity (Voltage difference per unit length)
Classification of metals based on conductivities:
Conductors
Insulators
Semiconductors

## Slide 4
Electronic and Ionic Conduction
Energy levels for a group of 12 atoms.

## Slide 5
Electronic and Ionic Conduction
Energy levels for a group of atoms.

## Slide 6
Electronic and Ionic Conduction
Example: Copper
Example: Magnesium
Example: Insulators
Example: Semiconductors

## Slide 7
Electronic and Ionic Conduction
For metals
For insulator or semiconductor

## Slide 8
Electron mobility in a crystal
An electron loses its kinetic energy as it moves across due to an external excitation source.
Drift velocity is used to describe the extent of scattering:
μe is called the electron mobility.
Conductivity , where n is the number of free or conducting electrons per unit volume and

## Slide 9
Electrical Resistivity of Metals
Matthiessen’s rule: overall resistivity of a metal is sum of the contributions from each of the factors – thermal, impurities and plastic deformation.

## Slide 10
Electrical Resistivity of Metals

## Slide 11
Semiconductivity
Intrinsic Semiconductors: Band gap < 2ev.
Examples: Si, Ge, GaAs, InSb

## Slide 12
Intrinsic Conductivity

## Slide 13
Intrinsic Conductivity
ni is the charge carrier concentration

## Slide 14
Extrinsic Semiconductors
n – type extrinsic semiconductor

## Slide 15
Extrinsic Semiconductors
n – type extrinsic semiconductor

## Slide 16
Extrinsic Semiconductors
p–type extrinsic semiconductor

## Slide 17
Temperature dependent Semiconductivity
Intrinsic semiconductor
Intrinsic semiconductor
n–type Extrinsic semiconductor
Intrinsic semiconductor

## Slide 18
Factors affecting the Carrier mobility
Influence of dopant concentration

## Slide 19
Factors affecting the Carrier mobility
Influence of Temperature

## Slide 20
Hall Effect
A magnetic field applied in the direction perpendicular to the direction of motion of a charged particle exerts force in the direction perpendicular to both the magnetic field and the direction of motion.

## Slide 21
Semiconductor Devices
Forward Bias
Reverse Bias

## Slide 22
Semiconductor Devices
Forward Bias

## Slide 23
Semiconductor Devices
Reverse Bias

## Slide 24
Semiconductor Devices
Input Voltage
Output Current

## Slide 25
The Transistor
Junction or Bimodal Transistors
Metal Oxide Semiconductors Field–Effect Transistor (MOSFET)

## Slide 26
The Transistor
Junction or Bimodal Transistors
Metal Oxide Semiconductors Field–Effect Transistor (MOSFET)
Schematic cross – section of MOSFET

## Slide 27
Electrical Conduction in Ionic Ceramics and Polymers
In ionic Ceramics, conduction of current takes place through electron and ionic motion.
Polyacetylene

## Slide 28
Dielectric Behaviour
Dielectric materials are insulators (non–metallic). Used in capacitors.
Capacitance, C = Q/V. Units are Farad.
In a parallel–plate capacitor with vacuum in between, , F/m.
In any other medium .
is the relative permittivity or dielectric constant.

## Slide 29
Field Vectors and Polarization
Dipole getting aligned along the direction of electric field – Polarization

## Slide 30
Field Vectors and Polarization
Surface charge per unit area or charge density D is given by,
D0 = ϵ0E in vacuum
D = ϵE for any dielectric material.
D is sometimes called dielectric displacement.
D = ϵ0E + P; P = ϵ0 (ϵr – 1)E

## Slide 31
Consider a parallel-plate capacitor having an area of 0.0006 m2 and a plate separation of 0.002 m across which a potential of 10 V is applied. If a material having a dielectric constant of 6.0 is positioned within the region between the plates, compute
The capacitance.
The magnitude of the charge stored on each plate.
The dielectric displacement D.
The polarization.
Field Vectors and Polarization

## Slide 32
Types of Polarization
Electronic Polarization
Ionic Polarization
Orientation Polarization
Electronic polarization that results from the distortion of an atomic electron cloud by an electric field.
Ionic polarization that results from the relative displacements of electrically charged ions in response to an electric field.
Response of permanent electric dipoles (arrows) to an applied electric field, producing orientation polarization.

## Slide 33
Frequency dependence of dielectric constant
An applied voltage of alternating direction

## Slide 34
Frequency dependence of dielectric constant

## Slide 35
Ferroelectricity
Spontaneous polarization – a dielectric analogue to ferromagnetism

## Slide 36
Piezoelectricity
Application of stress induces voltage. Applications–transducers, phonograph cartridges, speakers, audible alarms.