## Slide 1
Environmental Degradation of Materials
Dr. J. Venkatramani
219-B
venkatramani@iiitdm.ac.in

## Slide 2
Corrosion and Degradation of Materials
Stress Corrosion Cracking

## Slide 3
Corrosion and Degradation of Materials
Electrochemistry
Oxidation Reactions at Anode:
Reduction Reactions at Cathode:

## Slide 4
Corrosion and Degradation of Materials
Electrochemistry – Example: Corrosion of Zinc
Oxidation Reaction at Anode:
Reduction Reaction at Cathode:
Corrosion of Zinc
Total electrochemical reaction

## Slide 5
Corrosion and Degradation of Materials
Electrochemistry – Example: Rusting of Iron
Electrochemical reaction takes place in two stages

## Slide 6
Corrosion and Degradation of Materials
Concept of Electrode Potential
Not all metallic materials oxidize to form ions with same degree of ease.
Total electrochemical reaction

## Slide 7
Corrosion and Degradation of Materials
Concept of Electrode Potential
Not all metallic materials oxidize to form ions with same degree of ease.
Total electrochemical reaction

## Slide 8
Corrosion and Degradation of Materials
Standard EMF Series

## Slide 9
Corrosion and Degradation of Materials
Standard EMF Series
Total electrochemical reaction
With the overall cell potential of
ΔV0, given by,

## Slide 10
Corrosion and Degradation of Materials
Influence of Concentration and Temperature
Nernst equation:
R is the gas constant; T the absolute temperature; n is the number of electrons participating in either of the half cell reactions; and are molar concentrations and F is the Faraday constant = 96500 C/mol.
At 250C,

## Slide 11
Corrosion and Degradation of Materials
Problem: One-half of an electrochemical cell consists of a pure nickel electrode in a solution of Ni2+ ions; the other half is a cadmium electrode immersed in a Cd2+ solution.
If the cell is a standard one, write the spontaneous overall reaction and calculate the voltage that is generated.
Compute the cell potential at 250C if the Cd2+ and Ni2+ concentrations are 0.5 and 0.001 M, respectively. Is the spontaneous reaction direction still the same as for the standard cell?

## Slide 12
Corrosion and Degradation of Materials
Galvanic Series
– a more realistic and practical ranking

## Slide 13
Corrosion and Degradation of Materials
Quantifying corrosion rates
Corrosion penetration rate (CPR):
where W is the weight loss after exposure time t; ρ and A represent the density and exposed specimen area, respectively, and K is a constant, its magnitude depending on the system of units used.
Where, J is current density.

## Slide 14
Corrosion and Degradation of Materials
Prediction of corrosion Rates – Polarization
When the electrochemical reaction in not in equilibrium, there will be a difference between the emf generated and the standard emf. This difference is called overvoltage, denoted by η. The displacement of each electrode voltage potential from equilibrium is called Polarization.
Example: Zn cell connected to a standard cell, actual emf
Registered is – 0.621 V. Then,
η = – 0.621 – (–0.763) = 0.142 V

## Slide 15
Corrosion and Degradation of Materials
Prediction of corrosion Rates – Activation Polarization
The rate of reaction is controlled by the slowest step involved. This step has an activation barrier (energy) which has to be overcome.
J0 is the exchange current density.
Physical significance of J0: When the electrochemical reaction is at equilibrium for a standard half – cell, the rates of reduction (rred) and oxidation (roxid) are same and can be written as follows from the earlier definition of rate.

## Slide 16
Corrosion and Degradation of Materials
Prediction of corrosion Rates – Activation Polarization
Plot of overvoltage for Hydrogen electrode.
J0

## Slide 17
Corrosion and Degradation of Materials
Prediction of corrosion Rates – Concentration Polarization
Low reaction rates and high concentrations
High reaction rates and low concentrations

## Slide 18
Corrosion and Degradation of Materials
Forms of Corrosion
Uniform Attack
Galvanic Corrosion
Crevice Corrosion
Pitting Corrosion
Intergranular Corrosion
Selective Leaching
Erosion Corrosion
Stress Corrosion
Hydrogen Embrittlement

## Slide 19
Corrosion and Degradation of Materials
Forms of Corrosion
Uniform Attack
Galvanic Corrosion
Crevice Corrosion
Pitting Corrosion
Intergranular Corrosion
Selective Leaching
Erosion Corrosion
Stress Corrosion
Hydrogen Embrittlement

## Slide 20
Corrosion and Degradation of Materials
Forms of Corrosion
Uniform Attack
Galvanic Corrosion
Crevice Corrosion
Pitting Corrosion
Intergranular Corrosion
Selective Leaching
Erosion Corrosion
Stress Corrosion
Hydrogen Embrittlement

## Slide 21
Corrosion and Degradation of Materials
Forms of Corrosion
Uniform Attack
Galvanic Corrosion
Crevice Corrosion
Pitting Corrosion
Intergranular Corrosion
Selective Leaching
Erosion Corrosion
Stress Corrosion
Hydrogen Embrittlement

## Slide 22
Corrosion and Degradation of Materials
Forms of Corrosion
Uniform Attack
Galvanic Corrosion
Crevice Corrosion
Pitting Corrosion
Intergranular Corrosion
Selective Leaching
Erosion Corrosion
Stress Corrosion
Hydrogen Embrittlement

## Slide 23
Corrosion and Degradation of Materials
Forms of Corrosion
Uniform Attack
Galvanic Corrosion
Crevice Corrosion
Pitting Corrosion
Intergranular Corrosion
Selective Leaching
Erosion Corrosion
Stress Corrosion
Hydrogen Embrittlement

## Slide 24
Corrosion and Degradation of Materials
Corrosion Prevention
A judicious choice of materials depending upon the type of environment.
Changing the environmental conditions such as reduced fluid velocity, temperature; modifying the concentrations in the solutions
Use of inhibitors – depending upon the type of metal
Coatings
Cathodic Protection

## Slide 25
Corrosion and Degradation of Materials
Corrosion Prevention
A judicious choice of materials depending upon the type of environment.
Changing the environmental conditions such as reduced fluid velocity, temperature; modifying the concentrations in the solutions
Use of inhibitors – depending upon the type of metal
Coatings
Cathodic Protection